## Slide 1: Zirconia Based Stationary Phases for HPLC
Adriana Aceves and Emily Gorrie
December 9, 2014

## Slide 2: Outline
Introduction
Theory (Native, Modified)
Specific Applications (PBD, Carbon-coated)
Additional Applications
Conclusion

## Slide 3: Introduction
Silica is historically the first packing material used in column liquid chromatography
  Advantages:
    Well-known
    Available bonded or unbonded: able to separate wide range of analyte polarities
    Silica-polymer hybrids are very pH stable: 0-12
  Disadvantages:
    Slow equilibration
    pH sensitive (unless silica-polymer hybrid)
    Thermal instability
    Heterogeneous surface chemistry
Porous Graphitic Carbon
  More thermal stability than silica

## Slide 4: Introduction
Wanted something that would give similar separations as silica but with better stability
Porous graphitic carbon can be expensive and have poor mechanical stability
Exploration with inorganic supports
  ZrO2 (Zirconia)
  TiO2 (Titania)
  Al2O3 (Alumina)
  Other metal oxides
Originally developed for separating biomolecules
8

## Slide 5: Introduction
Zirconia
  Better thermal stability than silica; best of all metal oxides
  Stable from pH 1-14; best of laboratory tested metal oxides
  Stable up to 200oC: higher temperature means faster separation because lower pressure drop
  Similar efficiency to silica
  Amphoteric exchanger
  Lewis acid sites- allow for ligand exchange
9

## Slide 6: Theory
Formed by colloidal dispersion methods
  Particle size 3 to 10 µm have been made
  Methods available with narrow particle size distribution
Sample history determines many properties
  Crystallinity
  Surface Area
  Density
  Pore Size and Volume
11

## Slide 7: Theory
Crystallinity
  Properties depend on crystallographic form
    Amorphous
    Tetragonal
    Monoclinic
    Cubic
  Monoclinic most desired
    All zirconium cations are heptacoordinated to oxygen
    Difficult to get pure (usually mixture of tetragonal and monoclinic)
tetragonal
monoclinic
3,11

## Slide 8: Theory
Surface Area
  Strongly depends on thermal history:
    Treatment between 300 and 550oC results in sharp decrease in surface area
    Microcrystalline growth
    Intercrystalline sintering
  Less surface area per unit than silica
11

## Slide 9: Theory
Pore Size and Volume
  Temperatures higher than 200oC decrease pore volume (0.25 to 0.01 g/cm3)
  Much smaller pore volume than silica
Density
  Depends on the crystalline form
    Amorphous<Tetragonal<Monoclinic<Cubic
  Compensates for lower surface area vs silica
    30m2/g zirconia has surface area equivalent to 90-120m2/g silica
11

## Slide 10: Theory
More complex surface chemistry than silica
  Lewis Sites
  Bronsted Sites
  Greater surface heterogeneity
  Interaction with water
    Surface hydroxyls (Zr-OH, Zr µ-OH, Zr µ3-OH)
    Sigma coordinated water- allows for ligand exchange
Zirconia has extreme sensitivity to isomers and performs better than conventional anion exchangers when separating certain isomers
11

## Slide 11: Native Zirconia
Advantages
  Stability from pH 1-14
  Greater chemical stability
  “Tunable” surface area
  Easily cleaned (ie. with hot alkaline materials)
  High density allows for shorter columns
Disadvantages
  More complex surface chemistry than silica
  Hard Lewis bases such as carboxyl groups interact strongly with the zirconia surface resulting in extremely broad peaks
    CO2 must be removed from mobile phase
9,10,11

## Slide 12: Theory: Modified Zirconia
Complex chemistry can be advantageous
  Zirconia surface contains many adsorption sites and is able to ion and ligand exchange: modification is recommended
Amphoteric Exchanger: Anion exchanger in neutral and acidic solutions, cation exchanger in alkaline solutions
  Carbon Dioxide must be removed from mobile phase (blocks lewis acid sites)
11

## Slide 13: Modified Zirconia
Three classes of surface modification for zirconia
  Dynamic
    mobile phase with strongly interacting lewis base is used
    Fluoride
    Phosphate
  Permanent
    Bonded phases
    Hydrophobic quarternary amine
  Physical Screening (coating native zirconia with a polymer or carbon layer)
    Polymer Coatings
      Polybutadiene
      Polystyrene
      Polyethyleneimine
    Carbon Coated
8,11

## Slide 14: Modified Zirconia
Advantages
  Control some of the complex surface chemistry of bare zirconia
  Dynamic modification is easy to do in lab, recovery of bare column possible
  Retain the stability of native zirconia
  Homogeneous surface and good mass recovery possible
Disadvantages
  Additives to mobile phase may be undesired for certain samples
  Some polymer coatings do not fully coat the zirconia (heterogeneous surface)
10,11

## Slide 15: Application: PBD-Coated Zirconia
Bonded Phase
Thermally stable up to 150oC
Stable at high pressures up to 10,000 PSI
Relatively pH stable (2.2 to 12.0)
Mixed mode good for protein separations (cation exchange sites and hydrophobic interaction with PBD)
4,8,11

## Slide 16: Application: PBD-Coated Zirconia
Useful as a higher temperature reverse phase column
Benefits of high temperature chromatography:
  Faster Separations (retention time decreases with temperature)
  Increased Column Efficiency
4

## Slide 17: Application: PBD-Coated Zirconia
When elevated temperatures are used in combination with gradient elution techniques, the result is significantly increased elution efficiency
4

## Slide 18: Application: PBD-Coated Zirconia
Unlike silica, there is a minimal drift in retention times with the zirconia support
Explored as a reverse phase support with broad applicability
It was found that heating the column between runs can restore plate counts
Major Problem:
  Compounds with lewis base moieties strongly interact with any uncoated zirconia, which can result in peak broadening and tailing. These basic moieties can even irreversibly bind to the stationary phase.
  This can be counteracted by adding the base (ie. Phosphate, fluoride, carboxylate) to the mobile phase, but that is not always desirable.

## Slide 19: Application: Carbon-Coated Zirconia
Carbon supports are desirable
  Good selectivity for isomers and homologues
  Good chemical stability over a wide pH range
  Can use even higher temperatures than bonded phases
Drawbacks of typical carbon supports
  Poor mechanical stability
  Low surface area
  Heterogeneous surface (low loading capacity)
  Nonuniform pore structure
11

## Slide 20: Application: Carbon-Coated Zirconia
Carbon-coated zirconia
  Physical screening method
    Carbon deposited on zirconia surface via organic vapors at high T
  Good mechanical stability
  Can be heated over 500oC and good thermal stability over wide temperature range
  Stable at elevated pH (as with other zirconia phases)
  Excellent selectivity for polar, nonpolar, and isomeric compounds
  Able to cover approximately 97% of zirconia surface with carbon, which results in a more homogeneous surface, and reduced interactions between any lewis base moieties and the zirconia surface.
11

## Slide 21: Application: Carbon-Coated Zirconia
Application in amino acid separations
  Can avoid coelution
  Avoid low retention problems of traditional stationary phases
  Increased column lifetime (even with use of TFA)
  Lower efficiency vs. silica
Separation using Hypersil-ODS column (silica)
Separation using C/ZrO2
15

## Slide 22: Applications
Separation of polystyrene oligomers on carbon-clad zirconia- able to differentiate between very similar isomers (Sweeney, et al. Macromol. Chem. Phys. 2002, 203, 375-380).
Polyphosphate modified zirconia for purification of nucleic acid proteins- separation of single stranded DNA and RNA from double stranded DNA (Lorenz et al. Anal. Biochem. 1994, 216, 118-126).
Phosphated β-cyclodextrin modified zirconia monolith for chiral separation- separated 4 sets of enantiomers successfully (Park, J.; Park, J. J. Chromotogr. A. 2014, 1339, 229-233).
13,7,12

## Slide 23: Applications
C-18 column packed with polystyrene-coated zirconia porous particles- pharmokenetics studies for a new drug design in rat plasma. (Hsieh, Y.; Merkle, K. Rapid Commun. Mass Spectrom. 2003, 17, 1775-1780).
Polystyrene-coated zirconia- separated ibuprofen from related compounds and two decomposition products. (Kučera et al. J. Sep. Sci., 2005, 28, 1307-1314).
Magnesium-Oxide modified zirconia- used for HILIC to separate 7 basic compounds. (Wang et al. Talanta, 2014, 129, 438-447).
2,5,15

## Slide 24: Conclusions
Has some excellent advantages, including good chemical and physical stability, unique surface properties, and efficient separation capability
Useful for protein and biomolecules due to stability of zirconia under extreme conditions required
Surface modification makes zirconia based stationary phases applicable to a wider range of systems (good stability of modified phases as well)
Similar cost to analogous silica columns with good separation capability
Additional studies must be conducted in order to fully explore zirconia surface chemistry

## Slide 25: Other Considerations
Cost
9

## Slide 26: References (1)
Claessens, H.A.; van Straten, M.A. Review on the chemical and thermal stability of stationary phases for reversed-phase liquid chromatography J. Chromatogr. A. 2004, 1060, 23-41.
Hsieh, Y.; Merkle, K.; Wang, G. Zirconia based column high-performance liquid chromatography/ atomospheric pressure photoionization tandem mass spectrometric analyses of drug molecules in rat plasma Rapid Commun. Mass Spectrom. 2003, 17, 1775-1780.
Ikeno H; et al. Variation of Zr-L2,3 XANES in tetravelent zirconium oxides. J. of Phys.: Condens. Matter. 2013, 25 (16).
Kephart, S. T.; Dasgupta, P.K. Hot eluent capillary liquid chromatography using zirconia and titania based stationary phases Anal. Chim. Acta 2000, 414, 71-78.
Kučera, R.; Žižkovský, V.; Sochor, J.; Klimeš, J.; DOhnal, J. Utilization of zirconia stationary phase as a tool in drug control. J. Sep. Sci., 2005, 28, 1307-1314.
Li, J.; Hu, Y.; Carr, P.W. Fast separations at elevated temepratures on polbutadiene coated zirconia reversed-phase material Anal. Chem. 1997, 69, 3884-3888.
Lorenz, B.; Marme, S.; Muller, W.E.G.; Unger, K.; Shroder, H.C. Preparation and use of polyphosphate modified zirconia for purification of nucleic acids and proteins Anal. Biochem. 1994, 216, 118-126.

## Slide 27: References (2)
Nawrocki, J.; Dunlap, C.; Carr, P.; Blackwell, J. New materials for biotechnology: chromatographic stationary phases based on zirconia Biotechnol. Prog. 1994, 10, 561-573.
Nawrocki, J.; Dunlap, C.; McCormick, A.; Carr, P. Part I. Chromatography using ultra-stable metal oxide-based stationary phases for HPLC. J. Chroatogr. A. 2004, 1028, 1-30.
Nawrocki, J.; Dunlap, C.; Li, J.; Zhao, J.; McNeff, C.; McCormick, A.; Carr, P. Part II. Chromatography using ultra-stable metal oxide-based stationary phases for HPLC. J. Chromatogr. A. 2004, 1028, 31-62.
Nawrocki, J.; Rigney, M.P.; McCormick, A.; Carr, P.W. Chemistry of Zirconia and its use in chromatography. J. Chromatogr. A. 1993, 657, 229-282
Park J.M. Park J.H. Enantiomers separtions of basic chiral compounds by capillary electrochomotrography on a phosphasted β-cycloextrin-modified zirconia monolith. J. Chromotogr. A. 2014, 1339, 229-233.
Sweeney A. P, Wormell P, Shalloker A. End-Group Selectivity of low molecular weight polystyrenes on a Carbon clad zirconia stationary phase in reversed phase HPLC. Macromol. Chem. Phys. 2002, 203, 375-380.
Wang, Q.; Li, J.; Yang, X.; Xu, L.; Shi, Z.; Xu, L. Investigation on performance of zirconia and magnesia–zirconia stationary phases in hydrophilic interaction chromatography. Talanta, 2014, 129, 438-447.
Weber, T.; Jackson, P.; Carr, P. Chromatographic Evaluation of Porous graphitic carbon-clad zirconia microparticles. Anal. Chem., 1995, 67, 3042-3050.

## Slide 28: Additional Information: Theory, Native Zirconia
The thermal history of zirconia determines its physical properties
  Surface Area
    Increasing temperature decreases surface area
  Pore Size
    Higher temperature means loss of micropores (good)
    Higher temperature means more cylindrical pores (good for mass transfer)
  Mechanical Strength
    Higher temperature decreases strength